## Slide 1: Inovativni proizvodi i rješenja na bazi vapna za sanaciju povijesnih građevina
Davide Bandera, Mapei SpA, Italija
HRVATSKA KOMORA INŽENJERA GRAĐEVINARSTVA
Dani Hrvatske komore inženjera građevinarstva Opatija, 2018.
Davide Bandera
Notes: 1

## Slide 2
To solve the problems that affect a historical building and to address properly the remedial action it is necessary to carry out:
1. ANALYSIS
2. DIAGNOSTIC INVESTIGATIONS
3. CHOICE OF THE MATERIALS
4. DEFINITION OF THE APPLICATION METHODOLOGIES

## Slide 3
An analysis is necessary, since it is directed to collect historical data on the structure and information on the materials which compose the historical buildings and on their state of conservation
1. ANALYSIS

## Slide 4
MATERIALS DEGRADATION

## Slide 5
MATERIALS DEGRADATION

## Slide 6
MATERIALS DEGRADATION

## Slide 7
MATERIALS DEGRADATION

## Slide 8
MATERIALS DEGRADATION

## Slide 9
REDUCTION OF THE THERMAL COMFORT

## Slide 10
REDUCTION OF THE HYGIENIC COMFORT

## Slide 11
MOULDS AND ALGAE

## Slide 12
EFFLORESCENCES

## Slide 13
Through numerous and complex chemical analyses the diagnosis is used to evaluate the degradation state of the materials and to define its causes, in order to allow the restorers to act on the origin of the phenomenon
2. DIAGNOSTIC INVESTIGATIONS

## Slide 20
It is a very important operation, since the materials chosen should be both reversible and should respect the historical building which is going to be restored.
In short, these should be compatible with the original materials from a chemical, physical, mechanical and an elastic point of view
3. CHOICE OF MATERIALS

## Slide 22
Art. 3.9 Where possible, any measures adopted should be “reversible” so that they can be removed and replaced with more suitable measures when new knowledge is acquired
Art. 3.10 The characteristics of materials used in restoration work (in particular new materials) and their compatibility with existing materials should be fully established. This must include long-term impacts, so that undesirable side-effects are avoided
ICOMOS CHARTER

## Slide 23
  Art. 5.2 Particular attention has to be given to the compatibility between original and new materials
  Cements containing salts can only be used when there is no risk of damage to the masonry and particularly to its surfaces
  There may be a problem of leaching of soluble salts from the mortar resulting in efflorescence on the surface of brickwork
ICOMOS CHARTER

## Slide 24
- It depends on the type of product chosen, which has to be applied correctly according to the recommendations given by the producer
- If this is not followed, the results reached could be poor and the risk not to meet the required performances is rather high
4. DEFINITION OF THE APPLICATION TECHNIQUE

## Slide 25
    DEHUMIDIFYING RENDERS
    STRUCTURAL RENDERS
    TRANSPIRANT RENDERS
    INJECTION SLURRIES FOR THE RE-ADHESION OF RENDERS, ALSO FRESCOED, TO WALLS
    INJECTION SLURRIES FOR THE STRUCTURAL CONSOLIDATION
MAPEI MATERIALS FOR THE RESTORATION OF HISTORICAL BUILDINGS

## Slide 26
DEHUMIDIFYING RENDER

## Slide 27
Mortar based on lime and pozzolan
( San Francis Basilica Assisi – Italy )
MAPE-ANTIQUE mortar
( after 8 days )
CEMENT
Morphological Compatibility
Notes: This pictures makes a comparison between a pozzolanic mortar of the 13 th century and a mortar composed of Mapeantique after 8 days curing . As regards the morphology we don’t notice any particular difference between them and this is due to the fact that the lime that is present in Mapeantique reacts with all pozzolanic material with formation of calcium silicate

## Slide 28
Elastic mechanical incompatibility

## Slide 29
Elastic mechanical incompatibility

## Slide 30
ANSTETT test – Resistance to suluble salts
MAPE-ANTIQUE Binder
M-A Dehumidifying render
PRODUCTS NOT RESISTANT TO SULPHATES
Resistant to Salts
M-A products are resistant to the soluble salts and in particular to sulphates, which means that there is no chemical reaction

## Slide 31
Salt
Without porosity, the volume increment of the salt crystals can cause the failure
Macropores technology

## Slide 32
SUBFLORESCENCES

## Slide 33
Macropore
Macropores technology

## Slide 34
Evaporation
No degradation
Salt
Macropores technology
What can MACROPORE do?
The salt can crystallize in it

## Slide 35
Salt
Macropores technology

## Slide 36
MAPE-ANTIQUE Full system solution

## Slide 37
DEHUMIDIFYING RENDER Intervention procedure

## Slide 38
Removing the degraded render and washing carefully the surface

## Slide 39
Application of the scratch coat mortar

## Slide 40
Detail of the scratch coat mortar

## Slide 41
Application of the scratch coat mortar

## Slide 42
Application of the dehumidifying render

## Slide 43
Squaring of the dehumidifying render

## Slide 44
Levelling of the dehumidifying render

## Slide 45
Application of the scratch coat mortar
Positioning a
vertical guide
Planarization of the
vertical guide

## Slide 46
Application of the dehumidifying render by spray machine
Levelling of the dehumifying render with a straight edge
Removing the
vertical guide

## Slide 47
Filling of the voids after removing the vertical guide
Planing the surface of the dehumidifying render

## Slide 48
Construction site example

## Slide 49
Application of MAPE-ANTIQUE FC Ultrafine
< 100 µm

## Slide 50
Application of MAPE-ANTIQUE FC Ultrafine

## Slide 51
Smoothing of MAPE-ANTIQUE FC Ultrafine

## Slide 52
Application of MAPE-ANTIQUE FC Civile
400 µm

## Slide 53
Sponging MAPE-ANTIQUE FC Civile

## Slide 54
Sponging MAPE-ANTIQUE FC Civile

## Slide 55
Application of MAPE-ANTIQUE FC Grosso
700 µm

## Slide 56
Sponging MAPE-ANTIQUE FC Grosso

## Slide 57
Sponging the surface

## Slide 58
Application of the coloured finishing by float

## Slide 59
Sponging of the coloured finishing

## Slide 61
STRUCTURAL RENDER

## Slide 64
Applying the structural render

## Slide 65
Applying the structural render

## Slide 66
Squaring off the structural render

## Slide 67
Levelling off the structural render

## Slide 68
Applying the coloured finishing

## Slide 69
Applying the coloured finishing

## Slide 71
STRUCTURAL RENDER + MESH

## Slide 72
Particular of the structural renders + zinc plated mesh

## Slide 73
Fastening the glass fibers mesh

## Slide 74
Fastening the glass fibers mesh

## Slide 75
Fastening the glass fibers mesh

## Slide 76
Checking the gap between the mesh and the substrate

## Slide 77
with GLASS FIBERS MESH
with ZINC PLATED MESH

## Slide 78
with MAPENET EM 30 and MAPENET EM 40
with ZINC PLATED MESH

## Slide 83
Re-rendering with MAPE-ANTIQUE INTONACO NHL
HISTORIC CENTRE OF NEPI (VT)

## Slide 84
MUSEO SALINAS - PALERMO
3.2 RESTORATION
Renders reconstruction

## Slide 85
DEHUMIDIFING render
TRANSPIRANT render
TRANSPIRANT RENDER

## Slide 88
Transpirant base render based on natural hydraulic lime and
Eco-Pozzolan, for application on existing masonry, including that of historical interest and on new construction
  MAPE-ANTIQUE INTONACO NHL
  Transpirant render
MAPE-ANTIQUE line

## Slide 89
Continuous-feed rendering machine

## Slide 90
Creating new dehumidifying and transpirant renders with the products of
MAPE-ANTIQUE SILEXCOLOR and SILANCOLOR ranges
MUSEO SALINAS (PA)

## Slide 91
Application of MAPE-ANTIQUE INTONACO NHL

## Slide 93
Application of transpirant render

## Slide 94
Application of transpirant render

## Slide 95
Squaring the transpirant render

## Slide 96
Overview of an inside room

## Slide 97
Applying the coloured finishing

## Slide 98
Applying the coloured finishing

## Slide 99
Detail of SILEXCOLOR TONACHINO

## Slide 100
Overview of an inside room

## Slide 102
Outside overview

## Slide 103
Outside overview

## Slide 104
Outside pverview

## Slide 105
BASILICA OF ST. FRANCIS – ASSISI ( ITALY ) ( since year 1228 )
    INJECTION SLURRIES FOR THE RE-ADHESION OF RENDERS, ALSO FRESCOED, TO WALLS

## Slide 111
Reconstruction of the vaults with the masonry mortar

## Slide 112
Reconstruction of the vaults with the masonry mortar

## Slide 113
Reconstruction of the vaults with the masonry mortar

## Slide 115
Consolidation of the intrados with the slurry
By using this slurry there is no need to soak the masonry
It is suggested for consolidating frescoed renders
It is physically and chemically compatible with the masonry
It doesn’t react with a possible presence of soluble salts

## Slide 116
Consolidation of the intrados with the slurry

## Slide 117
Consolidation of the extrados with the slurry

## Slide 118
3.1 CONSOLIDATION
Re-establishing the renders adhesion

## Slide 119
    INJECTION SLURRIES FOR THE RE-ADHESION OF RENDERS, ALSO FRESCOED, TO WALLS
CAROVANA PALACE – HIGH SCHOOL PISA ( ITALY )

## Slide 120
Injection of the slurry ( super-fluid, salt-resistant, fillerized hydraulic binder )

## Slide 121
Injection of the slurry ( super-fluid, salt-resistant, fillerized hydraulic binder )

## Slide 122
    INJECTION SLURRIES FOR THE STRUCTURAL CONSOLIDATION
CAEN CASTLE – CAEN ( FRANCE )

## Slide 124
Mixing of the slurry

## Slide 125
Rubble masonries, cracks etc.

## Slide 126
Injection of the slurry ( super-fluid, salt-resistant, fillerized hydraulic binder )

## Slide 128
NEW

## Slide 129
MAPE-ANTIQUE
ECOLASTIC
Rivestimento bicomponente:
ELASTICO
PROTETTIVO
(resiste agli agenti atmosferici e ai raggi UV)
IMPERMEABILE
RESTISTENTE AI SALI
ESENTE DA CEMENTO
RESISTENTE ANCHE A SPINTA NEGATIVA (strutture interrate)
NEW

## Slide 135
PRIMA
DOPO

## Slide 136
TWO-COMPONENT COATING
ELASTIC
LIME BASED
CEMENT-FREE
SALT-RESISTANT
UV-RESISTANT
FOR WATERPROOFING AND PROTECTING CONSTRUCTION ELEMENTS, INCLUDING IN LISTED BUILDINGS

## Slide 137
DUCA DEGLI ABRUZZI COMPLEX – BARI ( ITALY )

## Slide 138
SAN PIERO A GRADO – PISA ( ITALY )

## Slide 139
CAROVANA PALACE – HIGH SCHOOL – PISA ( ITALY )

## Slide 140
PETRUZZELLI THEATRE – BARI ( ITALY )

## Slide 141
DOMUS AUREA – ROME ( ITALY )

## Slide 142
ANGIOINO CASTLE – COPERTINO ( ITALY )

## Slide 143
SALINAS ARCHAEOLOCICAL MUSEUM PALERMO ( ITALY )

## Slide 144
PEGGY GUGGENHEIM MUSEUM – VENICE ( ITALY )

## Slide 145
BARD FORTRESS – AOSTA ( ITALY )

## Slide 148
PALAZZO VECCHIO (rear facade) FLORENCE ( ITALY )

## Slide 149
PORTA BOZZOLO VILLA – CASALZUIGNO ( ITALY )

## Slide 150
PASSION ORATORY S. AMBROGIO BASILICA – MILANO ( ITALY )

## Slide 151
VILLA REALE – MILANO ( ITALY )

## Slide 152
BASILICA OF ST. FRANCIS – ASSISI ( ITALY )

## Slide 153
CARLO BRIDGE – PRAGA ( CZECH REPUBLIC )

## Slide 154
LIFE PALACE HOTEL, SIBENIK ( CROATIA )

## Slide 155
CLAY CASTLE – SIBIU ( ROMANIA )

## Slide 156
CLAY CASTLE – SIBIU ( ROMANIA )

## Slide 157
JESUIT FATHERS MONASTERY STARA WEIS ( POLAND )

## Slide 158
CAEN CASTLE – CAEN ( FRANCE )

## Slide 159
THANK YOU FOR YOUR ATTENTION
Archt. Davide Bandera Mobile +39 335 1303126
d.bandera@mapei.it